From: behanna@phoenix.syl.nj.nec.com  (Chris BeHanna)

Comprehensive Oil Article

Addressing the original question, which is better, Castrol GTX changed every 3,000 miles, or a synthetic oil changed at 3,000 or 5,000, or 7,000?

When it comes down to it, the extra cost (about $7/4 quarts vs $16/4 quarts) would be worth it, if there was a difference.

If you're operating under *severe* conditions, e.g., racing, then it might be worth it.  All that I have heard from people who have torn down motors beyond 80K is that if you change the oil and filter every 3K, then the crosshatch from the original factory cylinder honing will still be visible in the cylinder bores. Sounds like dead dinosaurs do the job just fine.

I must have missed the "conclusive" report posted earlier, so maybe it's time for a repost, or at least a followup discussion. 

From: carlp@frigg.isc‑br.com  (Carl Paukstis)

I don't believe in miracles, the Easter Bunny, or brand names.  I do tend to believe research chemist motoheads.  I use Castrol GTX 20w50, and change every 2500 miles.

Subject: Oil Question

Right, so where's Ed Hackett and his voluminous posting on oil when we need him?  Please, Ed, stem the flow of speculation and provide the factual additives to this discussion so we can filter out the truth from the myths.

First, I will answer a couple of questions asked by another.  Yes, it is OK to mix mineral and syntetic oils.  One of the early synthetics used was a Polyalkylene Glycol.  This was totally incompatable and would gel when mixed. This has not been used for years for automotive lubrication.  All common syntetics used for engine lubrication now days are a Polyalphaolefin (Mobil 1) or a Dibasic Organic Ester type (AMSOIL).  These are fully compatable with conventional oils.  In fact Golden Spectro and AGIP Sint 2000 are mixtures of mineral and synthetic oils.  It is always best to mix oils with the same rating (SG).  This insures that the additive packages are compatable and will maintain their effectiveness.

All engine oils use an organic Zinc compound  as an extreme pressure/anti wear additive.  Spectro adds more to their Motorcycle oil than to the car oil because Zinc is a poison to catalytic converters. You will also see that some "car" oil contains more than their motorcycle oil.  The difference in Zinc content between .11% and .16% is insignificant to the converter.  The little data I saw on the oils packaged by the motorcycle manufacturers indicated that they were no better than the top automotive oils.  While most were good, they didn't offer anything the cheaper oils do.  (They are in reality just repackaged and in some cases slightly reformulated top grade auto oils).

The following is a slightly modified repost of my original article. I have added a few bits that address some FAQs.  (long)


---------------------------------------

Choosing the best motor oil is a topic that comes up frequently in discussions between motoheads, whether they are talking about motorcycles or cars.  The following article is intended to help you make a choice based on more than the advertizing hype.

Oil companies provide data on their oils most often refered to as "typical inspection data".  This is an average of the actual physical and a few common chemical properties of their oils.  This information is available to the public through their distributors or by writing or calling the company directly.  I have compiled a list of the most popular, premium oils so that a ready comparison can be made.  If your favorite oil is not on the list get the data from the distributor and use what I have as a data base.

This article is going to look at six of the most important properties of a motor oil readily availiable to the public: viscosity, viscosity index (VI), flash point, pour point, % sulfated ash, and % zinc.

Viscosity is the measure of how thick an oil is.  This is the most important property for an engine.  An oil with too low a viscosity can shear and loose film strength at high temperatures.  An oil with too high a viscosity may not pump to the proper parts at low temperatures and the film may tear at high rpm.

The weights given on oils are arbitrary numbers assigned by the S.A.E. (Society of Automotive Engineers). These numbers correspond to "real" viscosity, as measured by several accepted techniques. These measurements are taken at specific temperatures. Oils that fall into a certain range are designated 5, 10, 20, 30, 40, 50 by the S.A.E.  The W means the oil meets specifications for viscosity at 0 F and is therefore suitable for Winter use.

The following chart shows the relationship of "real" viscosity to their S.A.E. assigned numbers.  The relationship of gear oils to engine oils is also shown.

_______________________________________________________________

|                                                             |

|      SAE Gear Viscosity Number                              |

|  ________________________________________________________   |

|  |75W |80W  |85W|    90        |        140             |   |

|  |____|_____|___|______________|________________________|   |

|                                                             |

|     SAE Crank Case Viscosity Number                         |

|  ____________________________                               |

|  |10| 20  | 30 | 40  |  50  |                               |

|  |__|_____|____|_____|______|                               |

______________________________________________________________

2  4  6  8  10 12 14 16 18 20 22 24 26 28 30 32 34 36 38 40 42

                 viscosity cSt @ 100 degrees C

Multi viscosity oils work like this:  Polymers are added to a light base(5W, 10W, 20W), which prevent the oil from thinning as much as it warms up.  At cold temperatures the polymers are coiled up and allow the oil to flow as their low numbers indicate.  As the oil warms up the polymers begin to unwind into long chains that prevent the oil from thinning as much as it normally would.  The result is that at 100 degrees C the oil has thinned only as much as the higher viscosity number indicates. Another way of looking at multi‑vis oils is to think of a 20W‑50 as a 20 weight oil that will not thin more than a 50 weight would when hot.

Multi viscosity oils are one of the great improvements in oils, but they should be chosen wisely.  Always use a multi grade with the narrowest span of viscosity that is appropriate for the temperatures you are going to encounter. The polymers can shear and burn forming deposits that can cause ring sticking and other problems. 10W‑40 and 5W‑30 require a lot of polymers(synthetics excluded) to achieve that range.  This has caused problems in diesel engines, but fewer polymers are better for all engines.  The wide viscosity range oils, in general, are more prone to viscosity and thermal breakdown due to the high polymer content. Very few manufactures recommend 10W‑40 any more, and some threaten to void warranties if it is used.  It was not included in this article for that reason.  20W‑50 is the same 30 point spread, but because it starts with a heavier base it requires less viscosity index improvers (polymers) to do the job.  AMSOIL can formulate their 10W‑30 and 15W‑40  with no viscosity index improvers but uses some in the 10W‑40 and 5W‑30.  Mobil 1 uses no viscosity improvers in their 5W‑30, and I assume the new 10W‑30. Follow your manufacturer's recommendations as to which weights are appropriate for your vehicle.

Viscosity Index is an empirical number indicating the rate of change in viscosity of an oil within a given temperature range. Higher numbers indicate a low change, lower numbers indicate a relatively large change.  The higher the number the better.  This is one major property of an oil that keeps your bearings happy. These numbers can only be compared within a viscosity range.  It is not an indication of how well the oil resists thermal breakdown.

Flash point is the temperature at which an oil gives off vapors that can be ignited with a flame held over the oil.  The lower the flash point the greater tendancy for the oil to suffer vaporization loss at high temperatures and to burn off on hot cylinder walls and pistons. The flash point can be an indicator of the quality of the base stock used.  The higher the flash point the better. 400 F is the minimum to prevent possible high consumption. Flash point is in degrees F.

Pour point is 5 degrees F above the point at which a chilled oil shows no movement at the surface for 5 seconds when inclined. This measurement is especially important for oils used in the winter.  A borderline pumping temperature is given by some manufacturers. This is the temperature at which the oil will pump and maintain adequate oil pressure.  This was not given by a lot of the manufacturers, but seems to be about 20 degrees F above the pour point. The lower the pour point the better. Pour point is in degrees F.

% sulfated ash is how much solid material is left when the oil burns. A high ash content will tend to form more sludge and deposits in the engine. Low ash content also seems to promote long valve life.  Look for oils with a low ash content.

% zinc is the amount of zinc used as an extreme pressure, anti‑ wear additive. The zinc is only used when there is actual metal to metal contact in the engine. Hopefully the oil will do its job and this will rarely occur, but if it does, the zinc compounds react with the metal to prevent scuffing and wear.  A level of .11% is enough to protect an automobile engine for the extended oil drain interval, under normal use. Those of you with high reving, air cooled motorcycles or turbo charged cars or bikes might want to look at the oils with the higher zinc content.  More doesn't give you better protection, it gives you longer protection if the rate of metal to metal contact is abnormally high.  High zinc content can lead to deposit formation and plug fouling.

The Data:

Listed alphabetically    ‑‑‑ indicates the data was not avaliable

Brand                    VI    Flash    Pour    %ash   %zinc

20W‑50
AMSOIL                  136     482     ‑38     <.5     ‑‑‑

Castrol GTX             122     440     ‑15     .85     .12

Exxon High Performance  119     419     ‑13     .70     .11

Havoline Formula 3      125     465     ‑30     1.0     ‑‑‑

Kendall GT‑1            129     390     ‑25     1.0     .16

Pennzoil GT Perf.       120     460     ‑10     .9      ‑‑‑

Quaker State Dlx.       155     430     ‑25     .9      ‑‑‑

Shell Truck Guard       130     450     ‑15     1.0     .15

Spectro Golden 4        174     440     ‑35     ‑‑‑     .15

Spectro Golden M.G.     174     440     ‑35     ‑‑‑     .13

Unocal                  121     432     ‑11     .74     .12

Valvoline All Climate   125     430     ‑10     1.0     .11

Valvoline Turbo         140     440     ‑10     .99     .13

Valvoline Race          140     425     ‑10     1.2     .20

20W‑40
Castrol Multi‑Grade     110     440     ‑15     .85     .12

Quaker State            121     415     ‑15     .9      ‑‑‑

15W‑50
Chevron                204      415     ‑18     .96     .11

Mobil 1                180      430     ‑55     ‑‑‑     ‑‑‑

Mystic JT8             144      420     ‑20     1.7     .15

15W‑40
AMSOIL                 135      460     ‑38     <.5     ‑‑‑

Castrol                134      415     ‑15     1.3     .14

Chevron Delo 400       136      421     ‑27     1.0     ‑‑‑

Exxon XD3              ‑‑‑      417     ‑11     .9      .14

Exxon XD3 Extra        135      399     ‑11     .95     .13

Kendall GT‑1           135      410     ‑25     1.0     .16

Mystic JT8             142      440     ‑20     1.7     .15

Shell Rotella w/XLA    146      410     ‑25     1.0     .13

Valvoline All Fleet    140      ‑‑‑     ‑10     1.0     .15

Valvoline Turbo        140      420     ‑10     .99     .13

10W‑30
AMSOIL                 142      480     ‑70     <.5     ‑‑‑

Castrol GTX            140      415     ‑33     .85     .12

Chevron Supreme        150      401     ‑26     .96     .11

Exxon Superflo Hi Perf 135      392     ‑22     .70     .11

Exxon Superflo Supreme 133      400     ‑31     .85     .13

Havoline Formula 3     139      430     ‑30     1.0     ‑‑‑

Kendall GT‑1           139      390     ‑25     1.0     .16

Mobil 1                ‑‑‑      430     ‑60     ‑‑‑     ‑‑‑

Pennzoil PLZ Turbo     140      410     ‑27     1.0     ‑‑‑

Quaker State           156      410     ‑30     .9      ‑‑‑

Shell Fire and Ice     155      410     ‑35     .9      .12

Shell Super 2000       155      410     ‑35     1.0     .13

Shell Truck Guard      155      405     ‑35     1.0     .15

Spectro Golden M.G.    175      405     ‑40     ‑‑‑     ‑‑‑

Unocal Super           153      428     ‑33     .92     .12

Valvoline All Climate  130      410     ‑26     1.0     .11

Valvoline Turbo        135      410     ‑26     .99     .13

Valvoline Race         130      410     ‑26     1.2     .20

5W‑30
AMSOIL                 168      480     ‑76     <.5     ‑‑‑

Castrol GTX            156      400     ‑35     .80     .12

Chevron Supreme        202?     354     ‑46     .96     .11

Exxon Superflow HP     148      392     ‑22     .70     .11

Havoline Formula 3     158      420     ‑40     1.0     ‑‑‑

Mobil 1                150      430     ‑65     ‑‑‑     ‑‑‑

Mystic JT8             161      390     ‑25     .95     .1

Quaker State           165      405     ‑35     .9      ‑‑‑

Shell Fire and Ice     167      405     ‑35     .9      .12

Unocal                 151      414     ‑33     .81     .12

Valvoline All Climate  135      405     ‑40     1.0     .11

Valvoline Turbo        158      405     ‑40     .99     .13

All of the oils above meet current SG/CD ratings and all vehicle manufacture's warranty requirements in the proper viscosity. All are "good enough", but those with the better numbers are icing on the cake.  The more expensive synthetics; AMSOIL, Mobil 1, and Spectro offer the only truly significant differences, due to their superior high temperature oxidation resistance, high film strength, very low tendancy to form deposits, stable viscosity base, and low temperature flow characteristics. Synthetics are superior lubricants compared to traditional petroleum oils.  You will have to decide if their high cost is justifed in your application.

The extended oil drain intervals given by the vehicle manufacturers (typically 7500 miles) and synthetic oil companies (up to 25,000 miles) are for what is called normal service.  Normal service is defined as the engine at normal operating temperature, at highway speeds, and in a dust free environment.  Stop and go, city driving, trips of less than 10 miles, or exterme heat or cold puts the oil change interval into the severe service category, which is 3000 miles for most vehicles.  Synthetics can be run two to three times the mileage of petroleum oils with no problems.  They do not react to combustion and combustion by‑products to the extent that the dead dinosaur juice does.  The longer drain intervals possible help take the bite out of the higher cost of the synthetics. If your car or bike is still under warranty you will have to stick to the recommended drain intervals.  These are set for petroleum oils and the manufacturers make no official allowance for the use of synthetics.

Oil additives should not be used.  The oil companies have gone to great lengths to develop an additive package that meets the vehicle's requirements.  Some of these additives are synergistic, that is the effect of two additives together is greater than the effect of each acting separately.  If you add anything to the oil you may upset this balance and prevent the oil from performing to specification.

The numbers above are not, by any means, all there is to determining what makes a top quality oil. The exact base stock used, the type, quality, and quantity of additives used are very important. The given data combined with the manufacturer's claims, your personal experience, and the reputation of the oil among others who use it should help you make an informed choice.

Ed Hackett                  The Desert Research Institute

edh@wheeler.wrc.unr.edu      Reno, Nevada   (702) 673‑7380

---------------------------------------------------------------------------------

